## Slide 1: The CBM Process for PCB
Peter Sjöbeck, CEO
peter.sjobeck@cuptronic.com
Mobile: +46 - 70 730 0000
Dr. Björn Atthoff, CTO
bjorn.atthoff@cuptronic.com
Mobile: +46 - 70 996 6118
Better HF properties, new materials.
Non confidential
Notes: My name is Peter Sjobeck and I come from a Swedish company called Cuptronic Technology.
Thank you for inviting me to give this presentation.

## Slide 2: Our unique solution
Easy to implement
Enhances performance
A new chemical process, an adhesion promotion,
for attaching metal on non-metallic materials
Notes: The CBM process (Covalent Bonded Metallization) is a revolutionary new way of attaching metals like Copper, Nickel, Silver and Gold to a variety of surfaces.
It is easy to implement, and enhances performance.
Today’s technologies for metal-adhesion to non-metallic surfaces rely mainly on mechanical adhesion by first creating a rough surface (down into the surface).
Current technologies have several issues, three of which being choice of materials, production cost and the use of Chrome+6 for etching.
The CBM process solves there problems.

## Slide 3: Covalent Bonded Metallization
The CBM© Process
1
2
3
4
Spray/dip
CBM chemicals
Expose to
UV light
Activated surface structures
Apply Palladium and electroless
Cu or Ni
Notes: The CBM process is very simple.
You apply the CBM chemical by spray or dip, and thereafter you expose it to UV light.
That is it.
Before you continue to standard Electroless Cu or Ni, you wash the pieces with cold water.

## Slide 4: CBM Process Adhesion vs Standard Adhesion
18 µm electroplated Cu
CBM Process (≈ 50 nm)
+ 0,1 µm electroless Cu
15 µm GX-13©
Etched standard base Cu

## Slide 5: CBM solves problems in many areas
Plating on Plastic
Allows for metallization on a wide variety of plastics in a multitude of shapes
Selective 3D metallization
No ablation, new materials
EMP/EMI shielding
Allows metalization on materials ranging from micrometer thick foils up to large 3D structures
New materials
Allows for metalization of a multitude of plastics
Replace metal to plastic
Allows the reduction of weight by replacing metals to plastics
PCB properties
Allows the production of very advanced circuit boards, high frequency, advanced patterns, narrow lines and spaces.

## Slide 6: Evaluated PCB materials
Plastic | Product name | N/cm | Lbs/in
Certain epoxy (HFFR4) |  | 15 | 8.6
PTFE | Taconic TLP 5 Taconic TLX 9 Nelco N9000 Rogers 3003 Rogers CLTE-MW | 25 >50 20 25 20 | 14.3 >28 11.4 14.3 11.4
LCP | Rogers Ultralam 3850 | 10 | 5.7
PI |  | 15 | 8.6
COC (Cyclic Olefin Copolymer) | transparent | 15 | 8.6
Peel Strength according to IPC-TM-650 2.4.8 (1 oz Cu), after solder float

## Slide 7: Evaluated Rogers PCB materials
Rogers base laminates | CBM technology peeltests (N/cm) | N/mm | Lbs/in
 | Initial values | After 20 s solder shock x3 | 105°C for 2 weeks
RO3003 | 20,2 | 16,3 | 9,6
RO3010 | 17,2 | 16,1 | 17,3
RO4835 10mil | 9,2 | 8,5 | 7,6
RO4835 10,7mil | 7,5 | 9 | 8,5
CLTE-AT RL | 13,9 | 13 | 15,6
CLTE-AT RT | 9,6 | 9,6 | 9,8
CLTE-AT ED | 10,3 | 17,2 | 10,8
RT/duroid 6002 | 25,3 | 26,1 | 26,8
RT/duroid 5880 | 22,5 | 22,6 | 14,3
TMM3 | 12,2 | 10,5 | 11,5
TMM4 | 11,1 | 11,3 | 12,9
TMM6 | 9,7 | 8.5 | 10
TMM10 | 8,9 | 8,6 | 9,4
TMM10I | 9,2 | 9 | 11,1
AS300C | 26,7 | 20,7 | 31,1
More or less base material breach
Only base material breach

## Slide 8: Evaluated POP materials. (several non-plating grade)
Plastic | Product name | N/cm | Lbs/in
PC/ABS | Cycoloy C1200 | 9 | 5.1
PC |  | 1 | 0.6
ABS | Novodur P2MC HI 121 H Recycled ABS: 50% LG TR558AI & 50% TERLURAN HI10 | 15 14 12 | 8.6 8.0 6.8
PLA filled with hemp | Trifilon Switch | 10 | 5.7
ASA |  | 13 | 7.4
PP |  | 30 | 17.1
PA 6 | Minlon 73M40 NC Grilon BS Natural Promyde B30 NC 100 Badamide B70GF30 | 40 40 20 20 | 22.8 22.8 11.4 11.4
PA 6,6 | Leona 91G60 | 15 | 8.6
PA 12 | Grilamid LV65H | 20 | 11.4
TR90 (PA) |  | 40 | 22.8
TPE |  | 20 | 11.4
PEI | Ultem 3452 | 8 | 4.6
Peel Strength according to IPC-650 and ASTM standard (1 oz Cu)
Notes: These are a few of the materials we have tested for different customers.
The list increases for every month.

## Slide 9: CBM Process features
“Simple” - Apply chemistry and UV light
CBM chemistry - Low cost
Applicable on a variety of new materials
Able to metallize very thin, and smooth substrates
High adhesion
Can be installed as parallel line, or other location

## Slide 10: PCB

## Slide 11: The CBM advantage
Metal adhesion technologies today are mainly mechanical and use dendrites to achieve adhesion to the surface.
The CBM® Process chemically alters the surface to enable electroless metal deposition, i.e. on a smooth surface.

## Slide 12: PCB: Better performance
As tracks shrink and frequencies rise, higher precison becomes key.
2020s
1970s

## Slide 13: PCB trace line manufacturing
Unit = µm
30
25
18
2
Conventional process
Using CBM Process
Using CBM Process results in better high frequency properties, due to no under etching and no “tabs” on Base copper holding the copper in place.

## Slide 14: CBM in surface and holes
Substrate
No teeth/tabs
Cuptronic process +
Electroless 0,2 µm Cu
Mechanically
attached 18 µm Cu
Electroplated Cu
Conventional process
Cuptronic process

## Slide 15: CBM in surface and holes
Rogers substrate after solder chock

## Slide 16: CBM in inter layer connection
Rogers substrate after solder chock

## Slide 17: Full Additive 3D with Laser - Solder
Soldering on PA-6
Picture by Laird Technology

## Slide 18: CBM in a PCB process
Drill panel
Pre-treatment of panel (if necessary, e.g. if hydrophobic)
Pre-wash
Drying
Application of Cuptronic chemistry (spray, dip, roll, conveyor)
Curing of Cuptronic chemistry (UV light conveyor)
Washing
Activation and reduction of palladium (or silver)
Electroless copper deposit
Drying
New equipment for
a PCB manufacturer

## Slide 19: Flow Diagram – conventional PCB process
Drilling of
through- and
blind holes
Electroless
Cu
Imaging
Exposing
Developing
Degreasing
Rinsing
Microetching
Rinsing
Acid dipping
Electrolytical
copper
plating
Rinsing
Acid dipping
Tin plating
Rinsing
Stripping
of dry film
Rinsing
Etching of
base copper
Rinsing
Stripping
of tin
Rinsing
Drying
Microetching of
conductors
Application of
soldermask
Further in
the process
18 µm

## Slide 20: Flow Diagram – with CBM Process
Drilling of
through- and
blind holes
Electroless
Cu
Imaging
Exposing
Developing
Degreasing
Rinsing
Microetching
Rinsing
Acid dipping
Electrolytical
copper
plating
Rinsing
Acid dipping
Tin plating
Rinsing
Stripping
of dry film
Rinsing
Etching of
base copper
Rinsing
Stripping
of tin
Microetching of
Conductors,
Incl. etching of Base Cu
Application of
soldermask
Further in
the process
Substrate without base Cu
CBM Process
grafting
≈ 0.1 µm Cu
Rinsing
Drying
eliminated

## Slide 21: Lab implementation of CBM Process
Application of CBM chemistry
Conveyorized R&D line for PCB 18 x 24 inch panels.
Application of CBM Process chemistry on both sides.
Capacity: 50,000 panels/month.

## Slide 22: Some Projects
Notes: I will now show four different projects utilising our CBM process

## Slide 23
RFS’s AllClear Antennas
Problem: 85% of building owners say no to antennas due to unsightly visuals.
Solution: Transparent Antennas with C.O.C. plastic.
Case

## Slide 24: RFS’s AllClear antenna installations

## Slide 25
AllClear Antennas RFS (Alcatel-Lucent)
Problem: 85% of building owners say no to antennas due to unsightly visuals.
Solution: Transparent Antennas made from C.O.C. plastic.
Case
Notes: RFS wanted to create a transparent antenna because 85% of the property owners in France did not want to continue to lease their properties to telecom companies for their mobile antennas because of visual pollution.
We help them find a transparent plastic which works very good with our CBM process.

## Slide 26
EMP/EMI Shielding (Samsung)
Problem: Thinner shielding materials.
Solution: Substitute textile EMI shielding (1 mm) with a metalized PET film (0.05 mm).
Case
10 µm PET film with 2 x 20 µm Cu
1 mm textile with Copper

## Slide 27
Plastic waveguides (Huber+Suhner)
Requirement: Reduce size, weight and cost of waveguides.
Solution: Metallized C.O.C plastic.
Case

## Slide 28
RFS/Alcatel, Lucent and others
Requirement: Reduce weight and decrease production cost.
Solution: Substitute metal components with metallized reinforced plastics.
RFS/Alcatel’s antennas
From metal to metalized plastic
RFS/Alcatel’s connectors
From brass to metalized plastic
Telecom - Air cavity filters
From aluminum to metalized plastic
(GE ULTEM® 3452)
Case

## Slide 29
Car door handles (SKODA)
Requirement: Wear and tear resistant metallized plastic without Cr(VI) etching.
Solution: CBM Process applied to reinforced plastic.
Case
Minlon® 73M40 NC - 40% mineral reinforced PA6
No restriction on the type of fillers in the polymer, allows for better mechanical properties.

## Slide 30
Selective metallization – 3D MID (LDS)
Requirement: Selective metallization on 3D parts
Solution: Either with UV-laser, Inkjet, or even better with Pad-printing.
Case
3 Methods
UV - Laser (apply CBM chemistry, design with laser)
Inkjet (apply design with Inkjet printer)
PAD printing (apply design with PAD printer)
Advantages
Cheaper materials with better properties can be used
Smooth surface under copper traces
Excellent edge definition
No creation of dust
E-less Copper lines on PA-6

## Slide 31
Selective metallization – 3D MID (LDS)
Requirement: Selective metallization on 3D parts
Solution: CBM process and activated (design) with UV-laser
Case
VIDEO

## Slide 32
Selective metallization – 3D MID (LDS)
Requirement: Selective metallization on 3D parts
Solution: CBM process and activated (design) with UV-laser
Case
Result of previous
VIDEO

## Slide 33
Selective metallization – 3D MID (LDS)
Requirement: Selective metallization on 3D parts
Solution: CBM process and activated (design) with UV-laser
Case
Multiple line widths
7 µm lines
CBM chemistry applied on whole surface and lines defined (activated) by laser.
Line width limited primarily by equipment used to define lines. Target is 1 µm lines.
Laser line definition process currently only implemented in lab environment.
Courtesy of Prof. Delsing,
Luleå University of Technology.

## Slide 34
Selective metallization – Sub 5 µm
Requirement: Sub 5 µm selective metallization
Solution: CBM process and activated (design) with UV-laser
Case
Double square SRR with strip line 3µm after copper metallization.
CBM chemistry applied on whole surface and lines defined (activated) by laser.
Line width limited primarily by equipment used to define lines. Target is 1 µm lines.
Laser line definition process currently only implemented in lab environment.
Courtesy of Prof. Delsing,
Luleå University of Technology.
Double circular SRR with strip line 3µm after copper metallization.

## Slide 35
Selective metallization – 3D MID (LDS)
Requirement: Selective metallization on 3D parts
Solution: Apply CBM chemicals via Pad-printing
Case
Method: Pad printing
Alternative to LPKF’s laser activation.
Applies CBM chemistry where needed and then activates it with UV flood light.
Advantages
Lower capital expenditure
Less complex machines
Off the shelf machines
High productivity
Good results on PTFE (25µm lines)
Pad printing machine

## Slide 36: Board members and key shareholders
Urban Fagerstedt | Chairman of the Board. Former VP R&D for Huawei Technologies Sweden and Senior Advisor to Huawei China. Urban has worked in the telecom industry 30 years. The last 15 years in development of cellular systems and in General Management positions for the last ten years.
Bo Westerberg | Board Member. Nötudden AB, Former VP at Ericsson, General Manager - Indelec (Spain), Plant Manager Philips, Senior Management Consultant - Maynard MEC AB and several Directorships.
Göran Lindahl | Former President and Chief Executive Officer at ABB, Ltd., Zurich, Switzerland, Currently member of the board of (among others) iGate Corporation (US), Patni Computer Systems Limited (India), Avinode Holding AB, LivSafe AB and IIT Board of Trustees (US, Chicago) - Previously member of the board of (among others) ABB, Anglo American, DuPont, Ericsson, Sony, Sony Ericsson, Ratos, Saab and, INGKA Holding BV (IKEA).
Hans-Göran Stennert | Board Member. IKEA Group, director of INGKA Holding BV (holding company for the IKEA Group) from 1993-2007. Chairman of the Board of INGKA Holding BV for the last ten years. Currently Chairman of the board of Eolus Vind AB.
Peter Sjöbeck | Board Member. CEO Cuptronic Technology AB,
Mikael Lövgren | Chairman of Bridgepoint's (private equity group) business in the Nordic regions. Prior to joining Bridgepoint in 2006, he spent twenty years with the Boston Consulting Group, as the founder and leader of its Nordic Operations and Nordic Healthcare Practice group. Mikael Lövgren currently sits on, among others, the board of the Karolinska University Hospital - a leading European hospital.
Notes: The company is owned by interesting private individuals.

## Slide 37: END

## Slide 38: EXTRA SLIDES

## Slide 39: Adhesion test example
Average Load/Width at average value (100 peaks and troughs) 26.1 N/cm
Average Load at average value (100 peaks and troughs) 16.6 N
Material: PA6 (Minlon 73M40), 25 µm Cu strip
Pull rate: 25.00 mm/min
Strip Width: 6.35 mm
Surface: Rz = 0,15 µm
Peel Test According to IPC 650 Standard

## Slide 40: CBM® visualized
Conventional processes
CBM process
0,3-0,7 μm Electroless Cu or Ni
Galvanic plating to desired level
Bare substrate
Polymer structure build-up
Activation and reduction of Pd

## Slide 41: Surface at the process steps
1
2
3
4
5
6
Bare substrate
CBM process application chemistry and exposure
Wash (water)
Palladium activation
Palladium reduction
Electroless copper

## Slide 42: Next Generation 3D – Full Additive 3D Process
3D Design freedom for other plastic materials
(same 3D as LDS, but greater material choice)
Any number of antennas in the cover without significant cost increase
E’less CU
process
Wash off
surplus
chemistry
Activate
selected
areas with
laser
Apply CBM
Chemistry
Surface
Treatment
(if necessary)
Plastic molding
Standard plastic
material incl.
glass fiber fillers

## Slide 43: LPKF’s LDS method (Not Cuptronic’c CBM process)
Molding
Laser Structuring
Plating
500x
Before Activation
After Activation
LPKF =
Mechanical adhesion

## Slide 44: Comparison Cuptronic vs LPKF
The Cuptronic process is different from the LPKF’s LDS process as no materiel is mixed into the plastic and that the laser is only used to activate the chemistry and not to ablate the surface.
These two differences will give the following advantages:
  Approx. 50% cost reduction of the plastic carrier compared to LDS material,
  No reduction in mechanical properties of plastic carrier (no limit on fillers)
  “No” color limitation
  Faster cycle times as a broader laser spot can be used and no z-axis correction is needed.
  Larger working volume without any need for Z-axis correction. Lower cost for laser optics.
  Much lower capital investments